## Slide 1
Machine Learning methods for a complete TGA analysis
Characterization of La1-xCaxNiO3±δ as catalyst precursors for dry methane reforming
Andres Marulanda-Bran
acamilo.marulanda@udea.edu.co
@marulandaandrec
Química de Recursos Energéticos y Medio Ambiente-QUIREMA., Instituto de Química, Universidad de Antioquia, Calle 70 no.52-21 Medellín, Colombia
Methodology
Results
Jose C-Salazar
jose.correas@udea.edu.co
@murderedhopes
Jaime Gallego
andres.gallego@udea.edu.co
@GallegoJaime_
Ea vs Ca content
(automatic from script)
Dry methane reforming reaction
In-situ CO2 TGA and XRD
Analytical framework: Fully-interpretable neuronal network
Conclusions
References
Arrhenius plot (automatic from script)
Interpretable neural networks were used to decompose and make sense of TGA data applied to key catalytic reactions, which allowed to estimate activation energies.
The non stoichiometry introduction of Ca into the material helps lower activation energies for key catalytical surface reactions.
A 0.3 Ca coefficient was found to be the most energetically efficient stoichiometry for CO2 reduction on the catalytic surface.
Reduced LaNiO3
…doped with Ca
Temperature (℃)
Weight (mg)
Ni
La2O3
CaO
Initial catalysts
~ 650
La2O2CO3
Ni
La2O3
Superficial lanthanum
oxycarbonate
~ 700
CaCO3
Massic calcium carbonate
Ni
La2O3
Ni
La2O3
~ 750
Carbonates decomposition
CO2 desorption
Ni
La2O3
Ni
La2O3
~250
Superficial adsorption
Ni
La2O3
Ni
La2O3
~ 850
CO2 adsorption
On Ni nanoparticles
Ni
La2O3
Ni
La2O3
~ 1180
CO2 decompostion
Ni oxidatiom
CO production
NiOx
La2O3
NiOX
La2O3
Reaction Model
Rackauckas, C. et al. Universal Differential Equations for Scientific Machine Learning. (2020).
Zhang, Q., Wu, Y. N. & Zhu, S.-C. Interpretable Convolutional Neural Networks. (2017).
Gallego, J. et al. React. Kinet. Mech. Catal. 119, (2016).
Problems such as multiple simultaneous chemical events make data analysis in chemistry a challenging issue. For that matter, more complex algorithms are needed to make sense out of the different processes behind these data. Machine learning brings powerful algorithms for data analysis, and their interpretability has recently been explored [1,2]. In this work we develop an interpretable-ML aided analytical framework for in-situ TGA process quantification, allowing us to estimate kinetic and thermodynamic parameters.
https://github.com/doncamilom/QuiremaTGADecomp